| Subject Code A19PC1CE14 |  |  |  |  |  |  |  |  | A19 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |

VNR VIGNANA JYOTHI INSTITUTE OF ENGINEERING AND TECHNOLOGY

(AUTONOMOUS)

B.Tech. III Year II Semester Regular Examinations, July, 2024

SOIL MECHANICS

(CE)

Time: 3 hours                                                                                			  Max. Marks: 70

Answer ALL questions in PART-A.

Answer any ONE question from each unit in PART-B.

PART-A

5X2=10M

|  | Give any two relationships using e, G, S, w and γ. | 2M | CO-1 | BL-2 |
| --- | --- | --- | --- | --- |
|  | For a given soil, liquid limit = 65%, plastic limit = 36%, Natural moisture content = 18%. Determine Liquidity and Consistency index. | 2M | CO-2 | BL-3 |
|  | What are the factors that affect permeability of soil? | 2M | CO-3 | BL-1 |
|  | Differentiate between Initial and secondary consolidation. | 2M | CO-4 | BL-2 |
|  | Write the merits and demerits of Direct shear test. | 2M | CO-3 | BL-2 |

PART-B

6X10=60M

| UNIT-I |  |  |  |  |
| --- | --- | --- | --- | --- |
|  | a) Explain the soil formation and brief about the types of soils based on deposition. b) A moist soil sample weighs 3.52N. After drying in an oven, its weight is reduced to 2.9N. The specific gravity of solids and the mass specific gravity are respectively 2.65 and 1.85. Determine the water content, void ratio, porosity, and the degree of saturation. Take γw=10kN/m3 | 5M 5M | CO-1 CO-1 | BL-2 CO-4 |
| OR |  |  |  |  |
|  | a) Explain how would you determine water content by oven drying method. b) In a compaction test on a soil, the mass of the wet soil when compacted in the mould was 1.855kg. The water content of the soil was 16%. If the volume of the mould was 0.945 litres, determine the bulk density, dry density, void ratio, degree of saturation, and percentage air voids. Take G=2.68 | 4M 6M | CO-1 CO-1 | BL-2 BL-4 |
| UNIT-II |  |  |  |  |
|  | Explain the unified soil classification in detail with all the soil groups available for coarse grained and fine-grained soils. | 10M | CO-2 | BL-3 |
| OR |  |  |  |  |
|  | a) Explain the plasticity chart for IS soil classification in detail with a neat sketch. b) Classify the soils A and B, with the properties as shown below, according to USC system Soil; WL, %; IP, %; % passing 4.75mm; % Passing 75microns. A; 45; 29; 100; 59. B; 55; 15; 100; 85. | 5M 5M | CO-2 CO-2 | BL-3 BL-4 |
| UNIT-III |  |  |  |  |
|  | How would you determine the average permeability of a soil deposit consisting of a number of layers in case of parallel and perpendicular flow? | 10M | CO-2 | BL-3 |
| OR |  |  |  |  |
|  | a) What is flow net? Describe all its characteristics in detail. b) The falling head permeability test was conducted on a soil sample of 4 cm diameter and 18cm length. The head fell from 1.0m to 0.40m in 20 minutes. If the cross-sectional area of the stand pipe was 1cm2, determine the coefficient of permeability. | 5M 5M | CO-2 CO-2 | BL-3 BL-3 |
| UNIT-IV |  |  |  |  |
|  | Plot the total, neutral and effective stress diagrams for the given conditions as shown in the figure. Take e=0.46 and G=2.65 | 10M | CO-3 | BL-3 |
| OR |  |  |  |  |
|  | The water table is located at a depth of 3m below the ground surface in a deposit of sand 11m thick. The sand is saturated above the water table. The total unit weight of sand is 20kN/m3. Calculate the Total pressure, Pore water pressure and Effective pressure at depths 0, 3, 7, 11m from the ground surface, draw the pressure distribution diagram. | 10M | CO-3 | BL-3 |
| UNIT-V |  |  |  |  |
|  | The following results were obtained from a standard compaction test on a sample of soil. Water Content, %; 12; 14; 16; 18; 20; 22. Mass of soil (kg); 1.68; 1.85; 1.91; 1.87; 1.87; 1.85. The volume of mould used was 950ml. Make necessary calculations and plot the compaction curve and obtain the MDD and OMC. Also calculate the void ratio, the degree of saturation and the theoretical MDD (G=2.70) | 10M | CO-4 | BL-4 |
| OR |  |  |  |  |
|  | a) Discuss the spring analogy for primary consolidation. what are its uses. b) A Normally consolidated clay layer 1.5 m thick is sandwiched between two sand layers. The average overburden stress at the middle of clay layer can be taken as 250 kN/m2. Due to construction of a structure, there is an increase in effective vertical stress of 90 kN/m2 at the middle of clay layer. The liquid limit of clay layer is 50% and the initial void ratio is 0.9. Estimate the primary settlement. | 5M 5M | CO-4 CO-4 | BL-3 BL-4 |
| UNIT-VI |  |  |  |  |
|  | a) What are the different drainage conditions available in triaxial test? Explain. b) An unconfined compression test was conducted on an undisturbed clay sample. The sample had a diameter of 37.5mm and length 80mm. Load at failure measured by proving ring was 28 N and the axial deformation at failure point was 13mm. Determine the unconfined compressive strength and the undrained shear strength of the clay. Plot all the results on a Mohr’s circle. | 5M 5M | CO-3 CO-3 | BL-3 BL-3 |
| OR |  |  |  |  |
|  | a) What is Mohr’s circle? Discuss its importance characteristics. b) Two identical specimens of a cohesionless soil were tested in a triaxial apparatus. The first specimen failed at a deviator stress on 1370 kPa under a cell pressure of 400 kPa. Determine the shear strength parameters. Also, find the deviator stress at failure when the cell pressure was 600 kPa. If the same soil is tested in a direct shear apparatus, estimate the shear stress at which the sample will fail under a normal stress of 600 kPa. | 5M 5M | CO-3 CO-3 | BL-3 BL-4 |

***